Deep mixing induced property changes in surrounding sensitive marine clays

more options

Author(s): Shen SL (Shen, Shui-Long), Han J (Han, Jie), Du YJ (Du, Yan-Jun)

Source: JOURNAL OF GEOTECHNICAL AND GEOENVIRONMENTAL ENGINEERING Volume: 134 Issue: 6 Pages: 845-854 Published: JUN 2008

Times Cited: 0 References: 27

Abstract: This paper presents a field study of installation effects of deep mixed columns on properties of the sensitive Ariake marine clay. Cone penetration tests were performed in the field to evaluate the change in the strength of the surrounding clay with time. Soil samples were taken before and after column installation to evaluate variations of physical, mechanical, and chemical properties of the surrounding clay. Test results indicated that the water content of the surrounding clay decreased while the concentration of cations increased as sampling locations approached the columns. Shear strength of the surrounding clay decreased during the installation but recovered after a short period of curing. Shear strength continued to increase with time over a period of 70 days. Based on the regression results, the surrounding soil after the installation of the columns took approximately 10 days to recover to the strength value before installation. On average, the shear strength of the surrounding clay increased over the original strength by approximately 23% after 40 days and 50% after 70 days, respectively. Discussion is presented on strength changes and key influence factors including soil disturbance and fracturing, thixotropy, consolidation, and diffusion of cations from deep mixed columns to the surrounding clay.

Document Type: Article

Language: English

KeyWords Plus: INSTALLATION

Addresses: Shen, SL (reprint author), Jiao Tong Univ, Sch Naval Architecture Ocean & Civil Engn, Dept Civil Engn, 1954 Hua Shan Rd, Shanghai 200030, Peoples R China Jiao Tong Univ, Sch Naval Architecture Ocean & Civil Engn, Dept Civil Engn, Shanghai 200030, Peoples R China Univ Kansas, Dept Civil Environm & Architectural Engn, Lawrence, KS 66045 USA SE Univ, Inst Geotech Engn, Nanjing 210096, Peoples R China

E-mail Addresses: slshen@sjtu.edu.cn

Publisher: ASCE-AMER SOC CIVIL ENGINEERS, 1801 ALEXANDER BELL DR, RESTON, VA 20191-4400 USA

IDS Number: 302LM

ISSN: 1090-0241

DOI: 10.1061/(ASCE)1090-0241(2008)134:6(845)